# E40 Designed joints in in situ concrete

### To be read with Preliminaries/General conditions.

### 120 CONSTRUCTION/ MOVEMENT JOINTS GENERALLY

- Accuracy: Position and form joints accurately, straight, well-aligned and truly vertical or horizontal or parallel with setting out lines of the building.

- Modifications to joint design or location: Submit proposals.

- Placing concrete to form movement joints:

  - Maintain effectiveness of joints. Prevent concrete entering joints or penetrating or impregnating compressible joint fillers.

  - Do not place concrete simultaneously on both sides of movement joints.

### 132A ADDITIONAL REQUIREMENTS FOR CONSTRUCTION JOINTS

- Limitations: minimum cover of 100mm.

### 230A PREPARATION OF CONSTRUCTION JOINTS

- Substrate: Uniform and free of dirt and debris

  - Remove surface irregularities.

  - Surface damage, cracks, holes and depressions: Repair with Newton 203-RM.

### 310A FLEXIBLE WATERSTOPS

- Manufacturer:  Newton Waterproofing Systems.

  - Product reference:  Newton 302 Injection Hose.

- Termination: Hose ends overlap. The overlap must be parallel and of 150mm with a 30-50mm gap between the two parallel ends.

- Placing concrete: Fully compact concrete around waterstops with no voids or porous areas.

### 540 INJECTION RESINS

Manufacturer: Newton Waterproofing Systems

Product reference: Newton 322-SP or Newton 323-SA