# J40 Flexible sheet waterproofing/ damp proofing

### To be read with Preliminaries/ General conditions.

### WORKMANSHIP SKILLS

- Operatives: Appropriately skilled and experienced for the type and quality of work.

- Use only Newton NSBC trained operatives. In Accordance with our BBA Certificate Newton CDM Solution is a specialist fit. The system should only be installed by installers who have been trained and approved by the Certificate holder. Newton Waterproofing Systems

- Registration: CSCS, CSSW, PCA

- Evidence: Operatives must produce evidence of skills/qualifications when requested

### MANUFACTURERS RECOMMENDATION/INSTRUCTION

- General: Comply with manufacturer’s printed recommendations and instructions current on the date of the Invitation to tender

- Changes to recommendations: Submit details

- Ancillary products and accessories: Use those supplied or recommended by Newton Waterproofing Systems Newton Specialist Basement

### 290A HIGH DENSITY POLYETHYLENE STUDDED CAVITY DRAIN MEMBRANE

- Substrate: Wide range of substrates in varying situations  Concrete, Brick, Concrete block, ICF, Fibran XPS 500-C

  - Preparation: May be required depending on substrate (Installation manual 3.1)

Manufacturer: Newton Waterproofing Systems.

  - System Reference Newton CDM System

  - Product reference: Wall membrane Newton 508 (M1R/M2R). – 2.4/2.07 x 20 m.

- Stud height: 8mm.

- Fixing: Mechanically fix walling sheets.

  - Fasteners: Newton MultiPlug (A1).

  - Fixing centres: Battens 400mm horizontal, 600mm vertical Curtain hung 500mm centres along the top edge of the wall membrane.

- Sealing: Rubber grommet on the Newton MultiPlug.

- Joints: Minimum 70mm.

  - Sealing: Flange joint - Newton WaterSeal Tape (A5), Stud into stud between last two rows of studs or Stud over stud joint - Newton WaterSeal Rope (A6).

- Drainage components: Newton Basedrain.

## WORKMANSHIP

### 310 WORKMANSHIP GENERALLY

- Condition of substrate:

  - Clean and even textured, free from voids and sharp protrusions.

  - Moisture content: Compatible with damp proofing/ tanking.

- Air and surface temperature: Do not apply sheets if below minimum recommended by membrane manufacturer.

- Condition of membrane at completion:

  - Neat, smooth and fully supported, dressed well into abutments and around intrusions.

  - Completely impervious and continuous.

  - Undamaged. Prevent puncturing during following work.

- Permanent overlying construction: Cover membrane as soon as possible.

### 360 JUNCTIONS WITH PROJECTING DPCS/ CAVITY TRAYS

- Adjoining surfaces: Clean and dry.

- Dpcs/ Cavity trays: Lap and fully bond/ seal with sheeting.

  - Laps (minimum):  50mm.

  - Bonding/ Sealing:  As drawing CDM-D14A-C.

### 365A JUNCTIONS WITH FLUSH DPCS/ CAVITY TRAYS

- Bring wall membrane past DPC: 50 mm minimum lap

- Sealing: Newotn MultiPlug

### 382A CAVITY DRAINAGE CHANNELS

- Manufacturer: Newton Waterproofing Systems.

  - Product reference: Newton Baseboard.

- Drainage components: Baseboard length (D12), Baseboard Outside Corner (D9), Baseboard Inside Corner (D10), Baseboard End Caps (Right/Left) D11R & (D11L), Baseboard Hanger (D12H), Baseboard Connector (D13)

### 384A CAVITY DRAINAGE PUMPS

- Manufacturer: Newton Waterproofing Systems.

  - Product reference: Newton CP or NP pumps.

- Type: Submersible.

- Flow rate: Pump dependant.

- Pumping head (minimum): Pump dependant.

- Discharge pipe size: 50mm.

### 386 CAVITY DRAINAGE SUMPS

- Manufacturer: Newton Waterproofing Systems.

  - Product reference: Titan-Pro.

- Size: Manufacturer's standard.